## Slide 1: L-J Model of Argon

## Slide 2: 12-6 form of Lennard-Jones potential

## Slide 3: L-J Model

## Slide 4: FCC or HCP?
 | Spacing Å | Energy cm-1
SC | 3.56 | -1132.4812
BCC | 3.52 | -1617.4023
FCC | 3.64 | -1712.5192
HCP | 3.64 | -1713.2478
0.00042

## Slide 5: Adding Noice to the lattice

## Slide 6: Using different potentials
BFW
HFD
0.00025

## Slide 7: Phonon Dispersion
FCC

## Slide 8: Phonon Dispersion
𝚪
𝚪
X
W
K
L

## Slide 9: Phonon Dispersion
𝚪
𝚪
X
W
K
L
123
184

## Slide 10: Sound Velocity
For small stress, strain is proportional (linearly varies with) strain ➢ Hooke’s law.
The proportionality constants are 4th order (rank) tensors.
Hooke’s law
Tensor form

## Slide 11: Elastic Constants
The total number of expected components are: 2D: 2×2×2×2 = 16 3D: 3×3×3×3 = 81. But, not all of these are independent.
➢ Cijkl = Cijlk (also, Sijkl = Sijlk) ➢ Cijkl = Cjikl (also, Sijkl = Sjikl) ⇒ only 36 of the 81 components are independent (for even the most general crystal)*.
From energy arguments it can further be seen that: Cijkl = Cklij (also, Sijkl = Sklij)* ⇒ of the 36 components only 21 survive (even for the crystal of the lowest symmetry).
All cubic crystals (irrespective of their point group symmetry) have only 3 independent components
⇒ Cijkl (or Sijkl)→ these are C1111, C1122, C2323.
This is further reduced in the case of isotropic materials to 2 independent constants (C1111, C1122).
Usually, these independent constants are written as E & ν.
Hence, for second rank tensor properties (like magnetic susceptibility, χij) cubic crystals are isotropic,
but, not for forth rank tensor properties like Elastic Stiffness.

## Slide 12: Elastic Constants

## Slide 13: Velocities
velocity ⍵/k of a longitudinal wave in the [100] direction is vs = (C11/⍴)1/2
velocity ⍵/k of a transverse wave in the [100] direction is vs = (C44/⍴)1/2

## Slide 14: Sound Velocity :: TODO